# WORK INSTRUCTION

# WI-1001 | Bracket Assembly Line | Rev A

Document No: WI-1001 | Date: 2025-01-15 | Revision: A

Department: Manufacturing | Line: Assembly-3

## 1. Scope

This Work Instruction defines the step-by-step process for assembling the bracket sub-assembly on Line Assembly-3, ensuring all quality, safety, and traceability requirements are met.

## 2. Required PPE

Safety glasses

Cut-resistant gloves

Steel-toe boots

## 3. Process Steps

| Step | Process | Machine | Instruction | Quality Check | Reaction Plan |
| --- | --- | --- | --- | --- | --- |
| 1 | Material Receiving | Vernier Caliper | 1. Collect material from incoming rack. 2. Verify material cert against purchase order. 3. Measure 3 samples with vernier caliper per drawing REV-C. 4. Record lot number in traceability log. | All dimensions within ±0.1 mm. Grade 4.6 cert present. | Quarantine lot. Raise NCR-Form-01. Notify SQE within 30 min. |
| 2 | Surface Preparation | Degreaser DT-01 | 1. Set degreaser tank to 60°C ± 5°C. 2. Immerse parts for 3 min. 3. Remove and blow dry with compressed air. 4. Inspect surface — no visible oil or contamination. | Visual inspection: clean, dry surface. Temperature log signed. | Stop, drain tank, re-clean parts. Call supervisor. |
| 3 | Spot Welding | SPM-01 | 1. Load part into fixture. 2. Set weld current per WPS-03. 3. Apply 12 spots per weld pattern drawing. 4. Verify electrode force 3.2–3.8 kN on gauge. 5. Mark part with chalk if first-off. | Pull test every 50 pcs. Nugget Ø 5.0–6.5 mm. Record in QC-Log-W. | Stop line. Check electrode tips. Perform 100% pull test on last 50 pcs. |

## 4. Rework Criteria

Parts failing visual or dimensional inspection shall be tagged RED and moved to rework area. Rework must be approved by QE before re-entry to line.

## 5. Related Documents

DRG-101 (Part Drawing)

WPS-03 (Weld Parameter Sheet)

QC-Log-W (Weld Quality Log)

NCR-Form-01 (Non-Conformance Report)